## Slide 1: MIT 3.071 Amorphous Materials 17: Glass Bridge
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Tempered vs. annealed glass

## Slide 3: Tempered vs. annealed glass
“When it’s lit on the side, then you can see faint stain marks.”

## Slide 4: Heat-strengthened / tempered glass
Glass heated to 600 – 650 °C and force-cooled to generate surface compression
ASTM C1048 standard
  Heat-strengthened glass: surface stress between 24 – 52 MPa, about twice stronger than annealed (untreated) glass
  Tempered glass: surface stress > 69 MPa (10,000 Psi), 4 to 5 times stronger than untreated glass
http://www.legardien.com/architectural-products
Notes: Tempered glass cannot be obtained by normal convective cooling (see previous slide).
Tempering methods: https://www.gage-glass.com/glass-tempering-method-n.html

## Slide 5: Strain-optical coupling: photoelasticity
“The experiments now described, furnish us with a method of rendering visible, and even of measuring the mechanical changes which take place during the compression, dilation, or bending or transparent bodies.”
Phil. Trans. R. Soc. Lond. 106, 156-178 (1816)
Sir D. Brewster

## Slide 6: Photoelastic coupling in materials
Nye, Physical Properties of Crystals, Oxford University Press, Oxford, UK (1957).
where
Strain:
Relative dielectric impermeability:
Photo-elastic tensor

## Slide 7: Photoelastic coupling in isotropic materials
where
Photoelastic birefringence
Shear photo-elasticity
Stress:
3 unknown parameters

## Slide 8: Photoelastic tensor measurement in thin films
Films coated on different substrates
Index as a function of temperature
Known CTE of film and substrates
Simulate stress distribution
Subtract thermo-optic contributions
Fitting to obtain photoelastic tensor
Appl. Opt. 49, 403 (2010)
Index measurement using prism coupling
Requires prior knowledge about the material
Limited accuracy

## Slide 9: Birefringence
Anisotropy of permittivity tensor: refractive index depends on the polarization direction of light
Refractive indices of α-quartz vs. wavelength
Double refraction

## Slide 10: Characterizing birefringence using polariscope
https://www.olympus-lifescience.com/en/microscope-resource/primer/lightandcolor/birefringence/

## Slide 11: Polariscope for photoelastic stress analysis
Optik 130, 213 (2017)

## Slide 12: Photoelastic stress analysis

## Slide 13: Tempered vs. annealed glass

## Slide 14: Mechanical strength of the glass bridge
F = 600 N
L = b = 1 m

## Slide 15: Mechanical strength of the glass bridge
Tensile strength of soda-lime glass
With compressive stress in tempered glass
One person
Two persons
Possible thickness of glass panels in Squid Games

## Slide 16: A more realistic case
Tensile strength of soda-lime glass
With compressive stress in tempered glass
F = 500 N
F = 2000 N