## Slide 1: MIT 3.071 Amorphous Materials 4: Phase Change Data Storage
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Phase change materials
Reset
Set
Amorphous
Crystalline
High electrical resistivity
Low electrical resistivity
Low optical reflectance
High optical reflectance

## Slide 3: Key performance metrics
Data retention
Programming speed
Recording density
Endurance (cycle lifetime)
Power consumption
Good glass stability
Fast crystallization
Size dependence of material properties, driver size
Electromigration and phase stability
Enthalpy of melting, heat capacity
Low thermal conductivity
Trade-off

## Slide 4: Ge-Sb-Te (GST) phase change alloy
GeTe4
Isostatic compositions
SbTe4
Phys. Rev. B 81, 174206 (2010);
Solid-State Electron. 111, 27 (2015).
Pseudo-binary alloy: (GeTe)x(Sb2Te3)y
  Main commercial composition
  Stressed rigid 3-D network
Fast switching compositions
  Ge15Sb85, Sb2Te
High thermal stability alloys
  (Ge2Sb1Te2)x(Ge)y
Amorphous: covalent
Crystal: resonant bonding

## Slide 5: Ge-Sb-Te (GST) phase change alloy
Phys. Rev. B 81, 174206 (2010);
Solid-State Electron. 111, 27 (2015).
Pseudo-binary alloy: (GeTe)x(Sb2Te3)y
  Main commercial composition
  Stressed rigid 3-D network
Fast switching compositions
  Ge15Sb85, Sb2Te
High thermal stability alloys
  (Ge2Sb1Te2)x(Ge)y
Sb2Te3
GeTe
Te
Ge
Sb
Amorphous: covalent
Crystal: resonant bonding

## Slide 6: Structure of cubic Ge2Sb2Te5 (225) alloy
Nat. Mater. 6, 824-832 (2007)
Adv. Mater. 32, 1908302 (2020)
Strong electron delocalization due to resonant (metavalent) bonding

## Slide 7: GeTe-Sb2Te3 pseudobinary phase diagram
Sb-rich liquid
Ge-rich solid
Noncongruent melting results in compositional segregation

## Slide 8: T-T-T diagram of GST phase change alloys
Emerging Non-Volatile Memories, Springer (2014)
Notes: Typical quench rate to get amorphous GST phase is 1E10 K/s

## Slide 9: Re-writable CDs and DVDs
Modulation of optical reflectance via laser-induced phase change

## Slide 10: Phase change memory (PCM)
  Discovery of threshold switching in chalcogenides
1968
Ovshinsky
  256-bit phase change memory demo
1970
Gordon Moore
  Discovery of rapid switching pseudo-binary GST material
1987
Yamada et al.
  Non-volatile phase change memory module commercialized
IBM, Micron, Samsung, …

## Slide 11: Phase change memory (PCM)
Electrodes used for both programming and read-out
Threshold switching: electric field driven bistability
  Transient behavior: electronic in nature, no structural change
  Contributes to reduced SET voltage
S. Hudgens and B. Johnson, MRS Bull. (2004); Phys. Rev. B 78, 035308 (2008).
Notes: Threshold switching mechanism: in Poole-Frenkel conduction, the electric field increases the probability of a carrier that occupies one trap to get to another one nearby. At low fields, this requires extended states. At the threshold field, however, also direct tunneling becomes possible, leading to the conductivity increase. Another model presumes that threshold switching stems from a field- and carrier density-dependent generation mechanism, thus providing a positive feedback once a critical field is attained. At low fields, however, recombination counterbalances the generation. There are various possible microscopic models that could account for this phenomenological effect such as impact ionization.

## Slide 12: Where does PCM stand against competitors?
https://news.hpe.com/beyond-dram-and-flash-part-2-new-memory-technology-for-the-data-deluge/

## Slide 13: 3D XPoint: a likely (?) PCM technology
https://www.intel.com/content/www/us/en/architecture-and-technology/optane-technology-animation.html

## Slide 14: Reversing engineering reveals…
Both the memory and the selector are based on chalcogenide alloys

## Slide 15
https://www.intel.com/content/www/us/en/products/docs/memory-storage/optane-persistent-memory/overview.html

## Slide 16: Applications beyond data storage: optics
Large optical property contrast in GeTe due to change of bonding type from crystalline (resonance) to amorphous (covalent) phase
Chem. Rev. 110, 240-267 (2010).

## Slide 17: Optical properties of Ge2Sb2Te5 (225) alloy
Amorphous state: low-index, reduced loss
Crystalline state: high-index, high loss
Data from Nat. Commun. 10, 4279 (2019)

## Slide 18: All-optical, multi-level on-chip memory
Nat. Photonics 9, 725 (2015)

## Slide 19: All-optical, multi-level on-chip memory
Optica 6, 1-6 (2019)

## Slide 20: Optical switching and non-volatile display
Optical switch
Nature 511, 206 (2014); Adv. Mater. 25, 3050 (2013)
Electronic paper display
Applications involving bistable states

## Slide 22
Nat. Commun. 12, 1225 (2021)

## Slide 23: Further readings
Phase Change Materials: Science and Application, Springer (2009)
  Google book link
Emerging Non-Volatile Memories, Springer (2014)
  Download link (MIT certificate required)
“Phase change materials and phase change memory,” MRS Bull. 39, 703 (2014)
“Designing crystallization in phase-change materials for universal memory and neuro-inspired computing,” Nat. Rev. Mater. 4, 150-168 (2019)