## Slide 1: MIT 3.071 Amorphous Materials 6: Glass Shaping
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 20
Introduction to Glass Science and Technology
  Ch. 13

## Slide 3
“Viscosity makes things happen essentially in slow motion. If you are trying to melt a crystalline solid (like ice or an aluminum oxide ceramic), as soon as you reach the melting point, a drop of liquid forms and falls away from the melting surface. Glass, on the other hand, … gradually transforms from a hard solid to a slowly softening liquid. This soft liquid gradually stiffens as it cools (because of its increasing viscosity), allowing glass blower time to shape and manipulate the glass.”
http://madsci.org/posts/archives/2007-09/1188944613.Ph.r.html
Crystal
Glass
Continuous viscosity-temperature curve

## Slide 4
“Viscosity makes things happen essentially in slow motion. If you are trying to melt a crystalline solid (like ice or an aluminum oxide ceramic), as soon as you reach the melting point, a drop of liquid forms and falls away from the melting surface. Glass, on the other hand, … gradually transforms from a hard solid to a slowly softening liquid. This soft liquid gradually stiffens as it cools (because of its increasing viscosity), allowing glass blower time to shape and manipulate the glass.”
http://madsci.org/posts/archives/2007-09/1188944613.Ph.r.html

## Slide 5: Viscosity reference points
h (Pa·s)
101
103
106.6
1012
1013.5
Melting point
Working point
Softening point
Annealing point (Tg)
Straining point
Glass blowing
Fiber drawing
Float glass
Lehr annealing
Working range
Pitch: 2.3 × 108
PGM
Chewing gum

## Slide 6: Basic properties of common silicate glasses
 | Soda-lime | Borosilicate | Fused silica
CTE (ppm/°C) | 9.2 | 3.2 | 0.5
Working point (°C) | 1005 | 1252 | N/A
Softening point (°C) | 696 | 821 | 1650
Annealing point (°C) | 510 | 560 | 1140
Strain point (°C) | 475 | 510 | 1070

## Slide 7: Early flat glass process: crown glass
Crown glass was produced by making a hole in a molten glass bubble, then spinning the glass to create a flat, circular sheet with a distinctive “bulls-eye” pattern

## Slide 8: Flat glass manufacturing: float glass process
Forming of a continuous ribbon of glass using a molten tin bath
  Melting and refining (homogenization and bubble removal)
  Float bath: glass thickness controlled by flow speed
  Annealing: stress release
  Inspection, cutting and shipping
102.5 Pa·s
1012 Pa·s
> 1015 Pa·s
101 Pa·s
Notes: A typical float-glass line produces 500-700 tons of glass per day, with the largest plants producing 1000 tons per day

## Slide 9
Notes: Glass cullets form an early liquid phase and help to expedite reactions between other raw materials

## Slide 10: Ultra-thin, ultra-wide glass by float stretching
Int. J. Appl. Glass Sci. 10, 275 (2019)
0.12 mm thick, 4 m wide float glass
Notes: The top surface shows a root mean square (RMS) roughness value of 1.81 nm. The RMS roughness of the bottom surface slightly increased to 3.57 nm.

## Slide 11: Flat glass manufacturing: down-draw methods
Preserves pristine surfaces: no subsequent polishing required
Broad range of thicknesses from millimeter to tens of microns
Mostly used for flat panel display glasses
© SCHOTT
Notes: THE LONG ROAD TO SUCCESS: FUSION DRAW GLASS: http://www.cmog.org/article/long-road-success-fusion-draw-glass

## Slide 12: Glassblowing
Gaffer
Blow pipe
Parison
Notes: Wall thickness uniformity

## Slide 13: Glass container production
Narrow-neck containers (e.g., bottles): blow-and-blow process
Wide-mouthed jars: press-and-blow process
http://www.beatsonclark.co.uk/
Notes: Avoids the frictional stick forces experienced by conventional shaping techniques by engineering the expansion of a parison such that substantially all of the lateral strain required to form the final article is accomplished prior to the outer surface of the parison contacting the surface of the shaping mold

## Slide 14: Glass container production
Notes: De-alkalization: use SO2 or SO3 to remove Na2O and CaO from glass surface to improve chemical resistance
Dual-end coating process:
Hot-end coating (> 450 C): thin (~ 10 nm) tin oxide to improve wear resistance and also adhesion of the polymer coating
Cold-end coating: (~ 100 nm) polymer to reduce friction and enhance scratch resistance; also acts as a diffusion barrier to mitigate aqueous chemical attack
https://www.lehigh.edu/imi/teched/GlassProcess/Lectures/Lecture10_Pantano_Surface_Treatments.pdf

## Slide 15: Glass caneworking
Zanfirico
Reticello
Millefiori

## Slide 16: Glass caneworking
Canes: thin glass rods (often with color); can be of a single color, or contain multiple strands arrayed in a pattern (murrine)
Basic glass work technique for adding intricate stripe patterns to glassware or blown glass
Gather glass with pontil
Gob shaping on marver
Cane drawing
Stack and bundle

## Slide 17
virtualglass.org

## Slide 18: Millefiori – “1,000 flowers”

## Slide 19: Stability of drawn cane structures
Are you breaking my lovely canes?
Scaling analysis
Scale-invariance of viscous flow: strain rate remains invariant if the externally applied stresses are kept constant regardless of system size
s
s
l-times system size
Same strain rate!
s
s

## Slide 20: Stability of drawn cane structures
F, s /l2
F, s
F, s
F, s /l2
l-times system size
Cane diameter D change:
Necking develops if viscosity is independent of diameter D
Are you breaking my lovely canes?

## Slide 21: Stability of drawn cane structures
F, s /l2
F, s
F, s
F, s /l2
l-times system size
Stability threshold:
Are you breaking my lovely canes?

## Slide 22: Stability of drawn cane structures
Now consider heat dissipation:
Radiative heat transfer dominates
Stefan-Boltzmann law
Temperature change rate
Viscosity dependence on temperature
Heat flux:
s = 5.67 × 10-8 W/m2K4
High T range
e : emissivity
Are you breaking my lovely canes?

## Slide 23: Modeling outcome
Assumptions:
Uniform temperature distribution along the cane cross-section
No heat or mass exchange between cane sections
Only considers radiative heat transfer from glass cane to the surroundings
Constant drawing speed
F
F
T1
T2
T1
T2

## Slide 24: Modeling outcome
Conclusions:
Thinner section cools faster
Viscosity increase in thinner section prevents necking
Cane diameter non-uniformity damps out
F
F
D1
D2
D1
D2
It works beautifully!

## Slide 25: 3-D glass printing

## Slide 26: Precision glass molding (compression molding)
Viscosity: 106.6 – 108 Pa·s; pressure: ~ MPa
Mold sticking and damage: TiN or SiC low friction coatings
Non-uniform temperature distribution
Post-molding deformation: thermal shrinkage, viscoelasticity
http://www.rpoptics.com/wp-content/uploads/2015/01/Precision-Glass-Molding-Technical-Brief_21.pdf
Notes: The mold material chosen must have a CTE that falls within an acceptable CTE range for the glass in use to avoid excessive thermal stress

## Slide 27
PGM glass asphere lens
LFW 47, 42-45 (2011)

## Slide 28: Making extremely large telescope mirrors
Corning Inc.
Image from Wikipedia

## Slide 29: Making extremely large telescope mirrors
© University of Arizona, Richard F. Caris Mirror Laboratory
Initial paraboloidal shape is formed by casting the mirror in the spinning furnace, followed by milling and polishing down to 25 nm accuracy
A honeycomb mirror structure leads to low weight and high stiffness
Notes: https://mirrorlab.arizona.edu/content/faq

## Slide 30: Mechanical properties of bulk metallic glass (BMG)
Absence of dislocations and slip planes/directions in BMG
  Large elastic limit and high yield strength (2% and 2 GPa in Zr-based BMGs)
  Poor global plasticity: absence of strain hardening, strong tendency towards shear localization
Cold working is not a viable processing solution
Polycrystalline metal
Amorphous metal
Grain boundaries
Crystal planes
Metals 3, 1 (2013)
Notes: Yield strength of A36 steel: 0.25 Gpa
Shear localization results from stress-coupling between shear transformation zones (STZs) and free volume redistribution
Shear localization leading to shear band formation is generally recognized to be a consequence of the absence of a strain-hardening mechanism, whereas strain softening due to the creation of free volume during the shearing precedes localization of shear.

## Slide 31: Mechanical properties of a commercial BMG
High yield strength, hardness, and elasticity
Data from Liquidmetal® Technologies

## Slide 32: BMG process design
Casting
Casting: suction casting, die casting
  Reduced volume shrinkage (< 1%): net-shape forming
  Cooling rate control: mold filling and crystallization mitigation
Data from Liquidmetal® Technologies

## Slide 33: BMG process design
Thermoplastic forming (TPF)
Thermoplastic forming: compression & injection molding, extrusion, rolling, blow molding, 3-D printing
  Thermal embrittlement: free volume decrease
Scripta Mater. 60, 160 (2009)
Notes: Typical viscosity values for TPF: injection molding 1E3 Pas, extrusion 1E7 Pas, blow molding 1E6 Pas

## Slide 34: BMG process design
Adv. Mater. 22, 1566 (2010)
Thermoplastic forming (TPF)
Glass-forming liquid fragility
  Liquids with low fragility have better temperature tolerance
Notes: Fragility varies widely among BMG formers; BMG has improved temperature tolerance in TPF compared to polymers due to their low fragility

## Slide 35: Compression molding
Adv. Mater. 22, 1566 (2010)
Sample size | Shape | Aspect ratio | Issues
mm to cm | Open structures | 1 to 10 | Mold release and mold wear

## Slide 36: Injection molding
Sample size | Shape | Aspect ratio | Issues
mm to cm | Open structures | 1 to 10 | Mold release and mold wear
Notes: Unlike MIM (metal injection molding), there are no debinding or sintering processes required after the injection

## Slide 37: Blow molding
Mater. Today 14, 14 (2011)
Sample size | Shape | Aspect ratio | Issues
10 mm to cm | Hollow shapes | 10 to 1,000 | Temperature control, mold sticking
Parison
Final shape
Notes: Typical maximum strain for traditional metals: 25%
Maximum strain of BMG is limited by onset of crystallization
Any unwanted temperature gradient within the blow-mold setup translates significantly faster into a temperature gradient in the BMG than in polymers

## Slide 38: 3-D printing of BMG
Mater. Today 21, 697 (2018)
Continuous softening behavior of BMGs enables extrusion-based 3-D printing through fused filament fabrication (FFF)

## Slide 39: 3-D printing of BMG
Mater. Today 21, 697 (2018)