## Slide 1: MIT 3.071 Amorphous Materials 7: Viscoelasticity and Relaxation
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 8, Ch. 13, Appendix A
Introduction to Glass Science and Technology
  Ch. 9 (does not cover relaxation)

## Slide 3: “The Nature of Glass Remains Anything but Clear”
“What don’t we know?” Science 309, 83 (2005)

## Slide 4
“There are more theories of the glass transition than there are theorists who propose them.”
David Weitz, Harvard University

## Slide 5: Is glass a solid or a viscous liquid?
V
T
Tm
Supercooled liquid
Glass
Solid
Elasticity
instantaneous, transient
Liquid
Viscosity
time-dependent, permanent
E : Young’s modulus
G : shear modulus
h : viscosity (unit: Pa·s or Poise)

## Slide 6: Structural relaxation in glass
T
Elastic regime
All mechanical and thermal effects only affect atomic vibrations
Viscoelastic regime
Glass structure and properties are history-dependent
Glassy state
Supercooled liquid
Viscous regime
Structural changes are instantaneous: equilibrium state can be quickly reached
V
Glass transition
Ergodicity breakdown

## Slide 7: Structural relaxation in glass
T
Viscoelastic regime
Glassy state
Supercooled liquid
Viscous regime
V
Glass transition
Deborah number (DN):
“… the mountains flowed before the Lord…”
Prophetess Deborah (Judges 5:5)
Elastic regime

## Slide 8: Viscoelasticity: complex shear modulus
Consider a sinusoidally varying shear strain
Elastic response:
Viscous response:
In a general viscoelastic solid:
G* : complex shear modulus
Shear/storage modulus
Loss modulus

## Slide 9: Phenomenological models of viscoelastic materials
Elasticity: Hookean spring
Viscosity: Newtonian dashpot
Models assume linear material response or infinitesimal stress
Each dashpot element corresponds to a relaxation mechanism
Notes: Refer to Appendix I in Vashneya’s book for a more rigorous treatment involving the concepts of dilatational and deviatoric components

## Slide 10: The Maxwell element
Serial connection of a Hookean spring and a Newtonian dashpot
Total stress:
Total strain:

## Slide 11: The Maxwell element
Constant stress (creep):
Constant strain (stress relaxation):
Relaxation time

## Slide 12: The Maxwell element
Oscillatory strain:
Notes: Energy loss per cycle: loss tangent; energy loss per unit time: 1/tau

## Slide 13: The Voigt-Kelvin element
Parallel connection of a Hookean spring and a Newtonian dashpot
Total stress:
Total strain:
Constant strain:
Constant stress:
Oscillatory strain:

## Slide 14: Generalized Maxwell model
…
For each Maxwell component:
Total stress:

## Slide 15: Generalized Maxwell model
…
Stress relaxation:
Prony series:
In real solids, a multitude of microscopic relaxation processes give rise to dispersion of relaxation time (stretched exponential)
Notes: When beta < 1, the stretched exponential can be written as a sum of exponentials with different decay time scales

## Slide 16: Elastic, viscoelastic, and viscous responses
Stress
t
Stress
t
Stress
t
Elastic strain
t
Viscoelastic strain
t
Viscous strain
t

## Slide 17: Viscoelastic materials
Mozzarella cheese
Human skin
Turbine blades
Volcanic lava
Memory foams
Naval ship propellers

## Slide 18: Boltzmann superposition principle
In the linear viscoelastic regime, the stress (strain) responses to successive strain (stress) stimuli are additive
t
t1
Stress
t
t1
Strain
t
t2
Stress
t
t2
Strain
t
Stress
t
Strain

## Slide 19: Boltzmann superposition principle
In the linear viscoelastic regime, the stress (strain) responses to successive strain (stress) stimuli are additive
t
t
Strain
Stress
Viscoelastic response is history-dependent
Relaxation function Y dictates time-domain response

## Slide 20: Comparing stress relaxation and structural relaxation
“Equilibrium” state
  Zero stress state
Driving force
  Residual stress
Relaxation kinetics
  Exponential decay with a single relaxation time
  Relaxation rate scales with driving force
V
T
“Equilibrium” state
  Supercooled liquid state
Driving force
  Free volume
Relaxation kinetics
  Exponential decay with a single relaxation time
  Relaxation rate scales with driving force

## Slide 21: Free volume model of relaxation (first order kinetic model)
V
T
Relaxation kinetics at constant temperature
Temperature dependence of relaxation

## Slide 22: Model predicted relaxation kinetics
Cooling rate: 10 °C/s
Varying reheating rate
10 °C/s
1 °C/s
0.1 °C/s
Slope: volume CTE of supercooled liquid

## Slide 23: Model predicted relaxation kinetics
Varying cooling rate
Reheating rate: 1 °C/s
100 °C/s
10 °C/s
1 °C/s
Fictive temperature and glass structure are functions of cooling rate

## Slide 24: Tool’s Fictive temperature theory
Fictive temperature Tf : the temperature on the supercooled liquid curve at which the glass would find itself in equilibrium with the supercooled liquid state if brought suddenly to it
With increasing cooling rate:
  Tf1 < Tf2 < Tf3
A glass state is fully described by thermodynamic parameters (T, P) and Tf
Glass properties are functions of temperature and Tf (structure)
Tf1
Supercooled liquid
Increasing
cooling rate
3
2
1
Tf2
Tf3
V, H
T

## Slide 25: Tool’s Fictive temperature theory
Glass property change in the glass transition range consists of two components
  Temperature-dependent property evolution without modifying glass structure
  Property change due to relaxation (Tf change)
Tf1
Supercooled liquid
V, H
Increasing
cooling rate
3
2
1
Tf2
Tf3
Volume:
Enthalpy:
Volume:
Enthalpy:
T

## Slide 26: Tool’s Fictive temperature theory
Glass property change in the glass transition range consists of two components
T
Tf1
Supercooled liquid
V, H
Increasing
cooling rate
3
2
1
Tf2
Tf3
Notes: With Tool’s equation, the first equation reduces to the free volume relaxation model

## Slide 27: Predicting glass structure evolution due to relaxation: Tool’s equation
T
Tf
P (V, H, S, etc.)
Supercooled liquid
Glass
Consider a glass sample with Fictive temperature Tf
Pg - Pe
Tf - T
Take time derivative:
Assume first-order relaxation:
Tool’s equation
Notes: Note that in general the relaxation time depends on Tf (in addition to its apparent dependence on T) as well!

## Slide 28: Tool’s Fictive temperature theory
J. Am. Ceram. Soc. 29, 240 (1946)

## Slide 29: Tool’s Fictive temperature theory
J. Am. Ceram. Soc. 29, 240 (1946)
Tool’s equation

## Slide 30: Difficulties with Tool’s Tf theory
Ritland experiment: two groups of glass samples of identical composition were heat treated to obtain the same refractive index via two different routes
  Group A: kept at 530°C for 24 h
  Group B: cooled at 16°C/h through the glass transition range
Both groups were then placed in a furnace standing at 530°C and their refractive indices were measured as a function of heat treatment time
Glass structure cannot be fully characterized by the single parameter Tf
J. Am. Ceram. Soc. 39, 403 (1956)

## Slide 31: Explaining the Ritland experiment
t
n
Structural relaxation in glass involves multiple structural entities and is characterized by a multitude of relaxation time scales
Tool-Narayanaswamy-Moynihan (TNM) model

## Slide 32: What is relaxation?
Finally done with my 3.071 project !

## Slide 33: Relaxation: return of a perturbed system into equilibrium
Examples
  Stress and strain relaxation in viscoelastic solids
  Free volume relaxation in glasses near Tg
  Glass structural relaxation (Tf change)
Time-dependent, occurs even after stimulus is removed
Debroah Number:
  DN >> 1: negligible relaxation due to sluggish kinetics
  DN << 1: system always in equilibrium
  DN ~ 1: system behavior dominated by relaxation

## Slide 34: Modeling relaxation
Maxwellian relaxation models
Boltzmann superposition principle in linear systems
Relaxation rate
Driving force

## Slide 35: Glass transition as a relaxation phenomenon: models
Free volume relaxation theory
Tool’s Fictive temperature theory
  Uses a single parameter Tf to label glass structure
  Tool’s equation (of Tf relaxation)
Structural relaxation in glass involves multiple structural entities and is characterized by a multitude of relaxation time scales
  The Ritland experiment