## Slide 1: MIT 3.071 Amorphous Materials 8: Mechanical Properties
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 18
Introduction to Glass Science and Technology
  Ch. 9

## Slide 3
Glass = fragile?
Material | Iron | Structural steel | Glass fiber
Ultimate tensile strength | 35 MPa | 550 MPa | 4890 MPa
Iron man
Glass

## Slide 4: Strength and toughness
Strength: applied stress a material can withstand
Toughness: energy absorbed by (work performed to) a material per unit volume before fracture
s
e
×
Linear limit
Elastic limit
Ultimate strength
Yield strength
W/V
s
e
×
Linear limit
W/V
Ultimate strength
Fracture strength

## Slide 5: Theoretical strength of a brittle material
W/V
s
s
s
e
sm
0
l
Theoretical strength is determined by the cohesive force between atoms
Work W performed to separate the solid equals to the energy of the fresh surfaces created during fracture

## Slide 6: Theoretical strength of a brittle material
W/V
When s << sm, s = E e
Work W performed:
Theoretical strength is determined by the cohesive force between atoms
Work W performed to separate the solid equals to the energy of the fresh surfaces created during fracture
s
e
sm
0
l

## Slide 7: Theoretical strength of a brittle material
Consider silica glass
  g = 3.5 J/m2, E = 70 GPa, a0 = 0.2 nm
Material | Glass | Silica glass | Silica nanowire
Ultimate tensile strength | ~ 30 MPa | 110 MPa | 26000 MPa†
Practical strength of engineering materials is much less than their theoretical strength
† “The Ultimate Strength of Glass Silica Nanowires,” Nano Lett. 9, 831 (2009)

## Slide 8: Griffith’s theory
Strength of practical materials is limited by stress concentration around tiny flaws (Griffith cracks)
s∞
s∞
Notes: In the case of a surface crack, a represents the full crack length

## Slide 9: Griffith’s theory
Strength of practical materials is limited by stress concentration around tiny flaws (Griffith cracks)
Stress concentration factor:
Fracture strength of a flawed material:

## Slide 10: Griffith’s theory
Strength of practical materials is limited by stress concentration around tiny flaws (Griffith cracks)
In flawed silica glass:
A. Griffith, “The Phenomena of Rupture and Flow in Solids,” Philos. Trans. Roy. Soc. London, A 221, 163 (1921)
Notes: The divergence between theoretical strength and experimental strength is usually ascribed to surface damage.

## Slide 11: Visualizing Griffith cracks in glass
Displacement field near a crack tip
AFM phase image
5 nm
Europhys. Lett. 89, 66003 (2010)
J. Am. Ceram. Soc. 94, 2613 (2011)
Water condensation at crack tip
Notes: Left image: a) and b) AFM images prior to and after deformation; c) theoretical calculation of displacement field; d) residual value of DIC analyzed displacement subtracted from c). The residuals are all less than approximately 0.2 nm, which is the order of atomic distances in the glass being studied, suggesting that at distances >10 nm from the crack tip, surface displacements surrounding the crack tip are elastic to within the experimental scatter given by the residuals of the measurement.

## Slide 12: Stress intensity factor and fracture toughness
Stress intensity factor (tensile):
Strain energy release rate (plane stress):
Fracture condition:
work of fracture
critical stress intensity factor
KIc is a material constant and is independent of crack length
Notes: The strain energy release rate is the energy dissipated during fracture per unit newly created fracture surface area

## Slide 13: Intrinsic plasticity in amorphous metals
Lack of global plasticity
Intrinsic plasticity
When G/B < 0.42: plastic; G/B > 0.42: brittle (G: shear modulus; B: bulk modulus)
As-cast Vitreloy-1
Annealed at 350 °C for 12 h
Phil. Mag. Lett. 85, 77 (2006)
5 mm
5 mm

## Slide 14: Intrinsic plasticity in amorphous metals
Phil. Mag. Lett. 85, 77 (2006)
G/B
G/B = 0.42
Fracture Energy (kJ/m2)

## Slide 15
Nat. Mater. 10, 123 (2011)
Crack tip in PdAgPSiGe BMG
Notes: Trade-off between yield strength and fracture toughness: diagonal lines show the plastic-zone size, Kc2/πσy2, where Kc is the fracture toughness and σy the yield strength.

## Slide 16: Brittle fracture of glass
When a crack exceeds the critical length, the crack becomes unstable and propagates catastrophically through the material
Glass cracking at 231,000 fps
Crack propagation velocity:
J. Am. Cer. Soc. 22, 302-307 (1939)
1540 m/s
Notes: Glasses are sensitive to surface defects

## Slide 17: Brittle fracture of glass
Ceramic Tech Today article link
Notes: In a perfectly brittle material stressed in tension, you could see crack propagation occurring at—or above—the speed of sound (sound velocity in glass ~ 5 km/s). But materials are rarely perfectly brittle and stressed in tension. It is more likely you will see crack propagation ranging between 0.01 to 4 kilometers per second, depending on strain-energy distribution.

## Slide 18: Fractography
Conchoidal fracture
Image from "Fracture analysis, a basic tool to solve breakage issues"
Notes: https://books.google.com/books?id=fzO2yCNxLioC&lpg=PP1&pg=PA103
The ratio of the fracture mirror radius to the critical flaw size has been found to be constant within a material. The ratio reported is 12.5 for fused silica and 10.0 for borosilicate glass.

## Slide 19: The fractured surface of glass
Peter L. Bocko, Cornell University / Corning Glass Technologies
Notes: Wallner lines, which result from the interaction between the propagating crack front and shear waves emanating from a secondary source, can be used to determine the crack speed, see for example: https://www.sciencedirect.com/science/article/pii/S1359645414005424

## Slide 20: The 4R rule
K. Hess, and C. Orthmann, Criminal Investigation, Cengage Learning (2016)
The 4R Rule: Ridge lines on Radial fractures are at Right angles to the Rear
Fracture propagation direction
Notes: Wallner lines are formed through an interaction of the crack front with stress waves and are perpendicular to crack propagation directions

## Slide 21: Static fatigue in glass
Under constant load, the time-to-failure varies inversely with the load applied in a logarithm scale
Sub-critical crack growth: crack length increases over time even when s∞ < sf
Universal static fatigue curve

## Slide 22: Stress corrosion
Reaction at crack tip:
Higher alkaline content generally reduces fatigue resistance
Higher susceptibility to stress corrosion in basic solutions
Thermally activated process
J. Non-Cryst. Solids 316, 1 (2003)
J. Am. Ceram. Soc. 53, 544 (1970)
Notes: Region I: thermally activated stress corrosion; Region II: kinetics limited by water transport to crack tip

## Slide 23: Fracture toughness measurement
ASTM Standard E1820-15: Standard Test Method for Measurement of Fracture Toughness
Standard specimen geometries to obtain load-displacement plot
Middle-cracked tension specimen
Compact tension specimen
Single edge-notched bend specimen (for three-point bending)
Eng. Fract. Mech. 85, 1 (2012)
Notes: All specimens shall be precracked by fatigue. Optical crack measurements are utilized to obtain both the initial and final physical crack sizes.

## Slide 24: Indentation of glass samples
Mechanical properties evaluated through indented crack size or crack-opening displacement based on empirical equations
Poor correlation with conventional test results can be a concern
J. Mech. Behav. Biomed. Mater. 2, 384 (2009)
Vickers indenter tip
Hertzian (sphere) indenter tip

## Slide 25: Indentation of glass samples
Vickers indentation of soda-lime glass
Loading, 50% Fmax
Loading, 100% Fmax
Unloading, 68% Fmax
Unloading, 11% Fmax
Unloading, 2% Fmax
Unloading, 0% Fmax
J. Am. Ceram. Soc. 73, 787 (1990)
Notes: The radial cracks are nucleated by flaws at the deformation zone boundary and are driven by the residual stress field arising from the strain mismatch of the plastically deformed zone (densified zone) embedded in the surrounding elastically restraining matrix.

## Slide 26: Fracture statistics
Experimental results of fracture strength can often be described by the Weibull distribution
The fraction F of samples which fracture at stresses below s is given by:
Probability density
  Probability of samples fracture at stress s
m : Weibull modulus

## Slide 27: Weibull plot
m : slope of the Weibull plot
s0 : intercept with horizontal axis
Mater. Res. Bull. 49, 250 (2014)
Notes: The fiber d1 yields two straight-line sections, indicative of a bi-modal distribution of flaws

## Slide 28: Summary
Theoretical and practical strengths of materials
  Practical strength of brittle materials is usually much lower than the theoretical strength due to the presence of defects
  Oxide glasses are extremely sensitive to surface defects
  Intrinsic ductility in select BMGs contributes to high toughness
Basics of fracture mechanics
  Griffith crack theory
  Fracture toughness
Fatigue and stress corrosion
Fracture toughness measurement
Fracture statistics: Weibull plot