## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 11: Photovoltaics
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: References
Physics of Semiconductor Devices
  Ch. 10
Solar cells: Operating Principles, Technology and System Applications
  Martin Green
Best Research-Cell Efficiency Chart
  NREL

## Slide 3: Photovoltaics (PV)
The average power incident upon the continental United States is ~ 500 times the national consumption
Broadband light source
Large area
Cost

## Slide 4: PV: a cost-effective renewable energy source
The cost of utility-scale solar is competitive with the marginal cost of coal, nuclear and natural gas

## Slide 5: Basic solar cell structure
I
V
ISC : short circuit current
Is : diode saturation current
0

## Slide 6: Other types of solar cells designs
Substrate
CuInSe2
All-back-contact c-Si cell
  Eliminates front contact shading
  Single-side contacts simplify cell stringing
Superstrate configuration
Substrate configuration
Thin film poly-crystalline cells
  CuInxGa1-xSe (CIGS)
  CdTe
  CuZnSnSe/S (CZTS)
250 mm

## Slide 7: Key performance metrics
Short circuit current: number of absorbed photons
I
V
solar spectral irradiance
quantum efficiency
0
solar cell area
Saturation current: semiconductor material quality
electron/hole lifetime
diffusion coefficients
intrinsic carrier density

## Slide 8: Key performance metrics (cont’d)
Open circuit voltage: split of quasi-Fermi levels
Energy conversion efficiency and Fill Factor (FF)
I
V
0
Differentiate with respect to voltage to obtain the maximum power:

## Slide 9: Efficiencies of different solar cells
“$1 per W Photovoltaic Systems,” DOE ARPA-E white paper

## Slide 10: Shockley-Queisser limit in single-junction cells
Energy loss mechanisms
  Sub-bandgap photon loss
  Carrier thermal relaxation
  Voltage VOC loss (eVOC < Eg)
  FF < 1
1)
2)
2)
3)
conduction band
valence band
1) and 2) only
Shockley-Queisser (S-Q) limit under one-sun illumination
W. Shockley and H. Queisser, J. Appl. Phys. 32, 510-519 (1961)

## Slide 11: Other efficiency limiting factors and mitigation
Carrier recombination
  Radiative recombination: photon recycling
  Non-radiative recombination: material quality improvement
Shunt resistance and series resistance
  Contact resistance reduction
  Processing optimization
Surface reflection
  Surface texturing
  Anti-reflection coatings
Poor band edge absorption
  Light trapping

## Slide 12: Impact of shunt and series resistance
Simulation results quoted from Pveducation.org

## Slide 13: Surface reflection mitigation
Reflectance on planar Si surface:
Surface texturing by anisotropic wet etching: multiple reflections increases absorption
Random texture on c-Si
Inverted pyramid texture
70.5°

## Slide 14: Light trapping: the Lambertian (4n2) limit
The upper limit for absorption enhancement factor in a thin film solar cell (with respect to single pass absorption) is given by 4n2
Assumptions
  Ergodicity
  Isotropic radiation
  Weak absorption limit
Inadequacies
  The ergodicity condition
  is violated in periodic
  grating structures
  Solar radiation has
  a small divergence
  angle of 0.534°
Isotropic scattering
d
Maximum absorption 4n2 × ad
J. Opt. Soc. Am. 72, 899 (1982)
Appl. Phys. Lett. 98, 011106 (2011)
Opt. Express 18, A366 (2010)
Opt. Express 20, A496 (2012)

## Slide 15: Understanding light trapping using wave optics
Cell
Diffraction couples light into waveguided modes in the solar cell slab
Waveguided modes leak back to free space when the phase matching condition is met
Absorption occurs during mode propagation
x
Consider a 1-D grating light trapping structure

## Slide 16: Understanding light trapping using wave optics
Consider normal incidence:
To reduce phase-matched leakage channels back to free space, the number of N’s satisfying the above condition should be minimized
To achieve maximal light trapping enhancement at l0, the grating period should be smaller than l0
Only one leakage channel N = 0

## Slide 17: Beyond the S-Q limit: spectrum splitting & tandem cells
X. Wang et al., Prog. Photovolt: Res. Appl. 20, 149-165 (2012).
J. McCambridge et al., Prog. Photovolt: Res. Appl. 19, 352-360 (2011).
Dichroic mirrors
Cells with band gap matched to the reflected bands
Cell 1
Cell 2
Cell 3
Eg1 > Eg2 > Eg3
Current matching:
  Since each sub-cell is connected in series, suitable band gaps must be chosen such that the design spectrum will balance the current generation in each of the sub-cells

## Slide 18: Tandem cell design example
N. Yastrebova et al., technical white paper: ”High-efficiency multi-junction solar cells: current status and future potential” (2008)

## Slide 19: Tandem cells mark the efficiency records

## Slide 20: Perovskite/silicon tandem solar cells
https://www.fluxim.com/perovskite-silicon-tandem-solar-cell-simulation

## Slide 21: Laterally arrayed multi-junction cells
Opt. Lett. 44, 3274 (2019)
No current matching constraint

## Slide 22: Concentrator photovoltaics (CPV)
Reduced capital expense for solar cells
Increased VOC with high photon flux
  Large carrier concentration increases
  the quasi-Fermi level separation
Fill factor boost
Capital investment for additional optics
Requires active tracking
Aggravated heating issue
“III-V multijunction solar cells for concentrating photovoltaics,” Energy Environ. Sci. 2, 174-192 (2009).
"Planar micro-optic solar concentrator," Opt. Express 18, 1122-1133 (2010).
Micro-concentrators

## Slide 23: Luminescent solar concentrators (LSC)
LSC: transparent slab embedded with luminescent emitters (organic dyes or quantum dots)
Luminescent light is waveguided in the LSC slab and eventually collected by solar cells mounted along the slab edge
Efficiency limiting factors: dye/QD re-absorption, luminescence leakage out of the escape cone
LSC with fluorescent emitters
Small, efficient solar cells
Leakage
Appl. Opt. 18, 3090 (1979)
Opt. Express 16, 21773 (2008)

## Slide 24: Beyond the S-Q limit: downconversion & upconversion
One high energy photon → multiple electron-hole pairs
  Multi-excitation generation: quantum dots
  Fluorescent downconversion: quantum cutting in rare earth ions
Two low energy photons → one electron-hole pair
  Upconversion: e.g. rare earth ions
  Two photon absorption
T. Trupke et al., J. Appl. Phys. 92, 1668 (2002).
B. Richards, Sol. Energy Mater. Sol. Cells 90, 1189-1207 (2006).
A. Shalav et al., Sol. Energy Mater. Sol. Cells 91, 829 (2007).

## Slide 25: Beyond the S-Q limit: thermophotovoltaics (TPV)
Thermal emitter
Spectral filter
Solar cell
Cell materials GaSb, Ge:
smaller band gap to capture photons from thermal emitter (T < 2000 K)
DBR filter
J. Appl. Phys. 97, 033529 (2005).

## Slide 26: From cell to system
System
https://www.samlexsolar.com/learning-center/

## Slide 27: PV cost reduction: where and how?
Balance of system (BOS) costs is the key to further solar system cost reductions

## Slide 28: List of symbols
I – electric current
V – voltage
Is – diode saturation current
kB – Boltzmann constant, 1.38 × 10-23 m2·kg·s-2·K-1
T – thermodynamic temperature
ISC – short circuit current
A – solar cell area
h – quantum efficiency
l / l0 – free-space wavelength
Eel – solar spectral irradiance

## Slide 29: List of symbols
ћ – reduced Planck constant, 1.055 × 10-34 J·s
w – angular frequency of light
ni – intrinsic carrier density
NA / ND – acceptor / donor concentration at the p / n side of a diode
Dn / Dp – diffusion coefficient of electrons / holes
tn / tp – electron / hole lifetime
Eg – band gap energy
e – elementary charge, 1.602 × 10-19 C
EFn / EFp – quasi-Fermi level for conduction / valence band

## Slide 30: List of symbols
VOC – open circuit voltage
P – output power
FF – fill factor
Pm – maximum power output
Vm / Im – voltage / current corresponding to maximum power output
RSH – shunt resistance
RS – series resistance
R – reflectance
n – refractive index of absorber material

## Slide 31: List of symbols
k0 – wave vector of incident light
kslab – wave vector of light trapped in the solar cell slab
kout – wave vector of light escaped from the solar cell slab
G – reciprocal lattice vector of light trapping gratings
L – period of light trapping gratings