## Slide 1
Grain boundaries and Complexions
Victor Venturi
JCD Leader
Notes: Main title: 40 pt. Arial
Presenter Name: 16 pt. Arial
Presenters Title: 16 pt. Arial Italic

## Slide 2: Outline
Initial motivation
Grain boundaries
  Brief Classification
  Coincidence Site Lattice
  0-lattice
Complexions
  Pure and non-pure materials
  Types of complexions and transitions

## Slide 3: Initial motivation
Classical MD indicates LLZO grain boundaries hinder Li motion
Yu, S., et al. “Grain boundary contributions to Li-ion transport in the solid electrolyte LLZO" Chem. Mater. 29 (2017).

## Slide 4: Initial motivation
Surface studies suggest LLZO grain boundaries allow for Li plating in the solid electrolyte!
Tian, H., et al. “Interfacial electronic properties dictate Li dendrite growth in solid electrolytes" Chem. Mater. 31 (2019).

## Slide 5: What is a grain boundary?
Physical perspective
  Interface between two grains of a crystal
    Note: the crystal on either side need not be of the same material
How to define this mathematically?
  First, define boundary by its normal vector
  Next, define relative grain misorientation
  How many variables are needed to fully describe a GB?
    Geometric: 5
    Thermodynamic: ( is the number of components)
    Total of (not accounting for translations along and orthogonal to the boundary)
*There are other ways to define the misorientation vector (such as quaternion), but for simplicity, we will stick with

## Slide 6: How to classify GBs?
Total magnitude of
  Small angle
    Frank’s formula (simple):
  Large angle
Relative orientation of and
  Pure tilt:
  Pure twist:
Source: Slinky Puppet
* In theory, is the Burgers vector of the DSC lattice, but small CSL
Combination is a “general” GB

## Slide 7: Special cases: CSL
Normally, regions along the GB where the crystals “disagree” increase the overall energy of the GB
  One way to decrease this energy is by having atoms along the GB that are undisturbed in both sides of the boundary
Coincidence Site Lattice (and Displacement Shift Complete interlude)
  Super-lattice composed of lattice points of both interpenetrating crystals that occupy the same position in space
  Generally, ratio between volume of CSL and original crystal given by

## Slide 8: CSL energies for Cu
Monzen, R., et al. "Correlation between the boundary energy and precipitation in copper-[011] symmetric tilt boundaries." (1990).

## Slide 9: 0-lattice theory
Transformation from crystal 1 to crystal 2 with :
The points in each crystal can be binned into classes based on their internal coordinates (in each lattice):
A coincidence site happens when
Some interesting aspects I will not talk about:
  Different matrices can give origin to same crystal 2; which to pick?
  What happens when rank?
  The “birth” of DSC
Bollmann, W. "Crystal Defects and Crystalline Interfaces, 1970." (1982).
Notes: Bollmann also shows that the choice of origin does not matter

## Slide 10: 0-lattice closing comments
Pros
  Fully mathematical
    If you know the “misorientation” between the two crystals, you know what the ideal boundary looks like
    Constructing GB for simulations becomes simpler
  Formal introduction of DSC
Cons
  From a computational standpoint, some 0-lattices can be too large
  Small changes in matrix yield different 0-lattices, but that is not realistic.
  Real grain boundaries rarely look ideal

## Slide 11: Grain boundary “phases”
At the interfaces between grains, new phases, sometimes different from bulk, can form
  These new phases are commonly called complexions
  They can exhibit phase-like transitions in their structure and chemistry
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 12: Complexions in pure materials
Congruent transitions (rare)
  No change in geometrical parameters of GB
Non-congruent transitions
  Faceting: maintains the misorientation , but forms different inclinations
Non-congruent transitions
  Dissociation: creates two GBs separated by a bulk phase;
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).
Notes: Dissociation is also called wetting!

## Slide 13: Complexions in non-pure materials
Adsorption/Segregation Langmuir-McLean model
  Fixed number of adsorption sites per unit area
  GB is an entity in equilibrium with bulk
  GB is a regular solution with interaction
  Strong adsorbate-adsorbate attraction 1st order phase transition
    This is exactly the same as a regular solution!
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 14: Complexions in non-pure materials
Prewetting
  Introduction
    Fixed wall:
      perfect wetting by
    Three phases in contact
Cahn, J. W. “Critical point wetting" J. Chem. Phys. 66 (1977).

## Slide 15: Complexions in non-pure materials
Prewetting: Cahn model / Critical Point Wetting – CPWT
  Material with a miscibility gap between phases and
  Planar surface at ; short-range interaction energy with material given by . Excess free energy of surface given by
  is the bulk composition
  is the energy needed to create a unit volume with composition from a reservoir at

## Slide 16: Complexions in non-pure materials
Prewetting: Cahn model / CPWT
  is minimized when
  At interface:
  Assume
  Getting a better feel for what this all means…
Notes: The condition at the interface is called a ”natural condition”; it boils down to a force balance

## Slide 17: Complexions in non-pure materials
Prewetting: Cahn model / CPWT
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 18: Complexions in non-pure materials
Prewetting: Cahn model / CPWT
  At incoherent GB between solid phases with lattice mismatch, CPWT fails because it does not account for strain energy
  Only considers short-range interactions at the surface:
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 19: Complexions in non-pure materials
Premelting: Kobayashi-Warren-Carter (KWC)
  Surfaces and interfaces melt at lower temperature than bulk
  Melting can be understood as a special case of wetting
  Mean-field modeling: excess free energy of planar GB at
    is a measure of crystallinity; is a perfect crystal
    measures grain misorientation
    is the penalty of a misorientation, with ;
  But is minimized when is a step function at !
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 20: Complexions in non-pure materials
Premelting: KWC
  This is very similar to CPWT!!
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 21: Complexions in non-pure materials
CPWT (composition) + KWC (order-disorder)
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 22: Complexions in non-pure materials
Discrete complexions: Dillon-Harmer
  Experimentally observed GBs with discrete thicknesses
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 23: Complexions in non-pure materials
Discrete complexions: Dillon-Harmer
  Colloidal theories suggest
  Beyond a certain point, the barrier to increase the thickness is so small we can consider these complexions as continuous but finite inter-granular films
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 24: Complexions in non-pure materials
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 25: Complexions in non-pure materials
Dillon-Harmer “shortcomings”
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 26: Complexions in non-pure materials
Final remarks
  GB complexions formation and transitions are quite complex and material dependent, and this not accounting for:
    Directional bonds
    Cations and anions
    Electrostatic space charge
    van der Waals interactions
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 27: Complexion diagrams
How to represent a phase diagram when there are variables?
  Holding all geometric parameters constant, this becomes similar to a phase diagram
  Overlay bulk and complexion diagram
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 28: Complexion diagrams
Thermodynamic approach
  Here, only for quasi-liquid complexions
  Stability when
  Relative interfacial energy can be expressed as
  Maximum thickness of quasi-liquid inter-granular film
partial order and gradient
other interfacial interactions
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).
Notes: is the excess free energy of “dry” GB without any complexion
𝛾_𝐺𝐵^0 is the excess free energy of “dry” GB without any complexion

## Slide 29: Complexion diagrams
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 30: Complexion terminology
Transitions
  Geometry
    Congruent vs. Non-congruent: do or change?
    Structural: ) held constant and change; atomic structure changes
    Faceting: changes but does not
    Dissociation/wetting: changes but does not
  Order/composition
    Prewetting: nanolayer of different composition forms near wetting
    Premelting: disordered liquid-like structure below melting point
    Adsorption: dramatic change in solute adsorption
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 31: Complexion terminology
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 32: Complexion terminology
Types
  Composition
    Intrinsic: pure material, complexion composition equal to bulk, but density might be different
    Extrinsic: non-pure material; complexion composition usually different from bulk
  Thickness (and composition)
    Dry (clean; monolayer), Moist (bi/tri/nanolayer), Wet (bulk film)
  Periodicity
    Ordered vs. Disordered
Cantwell, P. R., et al. “Grain boundary complexions" Acta Materialia 62 (2014).

## Slide 33: How can complexions affect the material?
Embrittlement
GB mobility and abnormal grain growth
Diffusivity along complexion
  Empirical observation:
Some evidence that complexions can affect electrical, thermal, optical, chemical, and magnetic properties
  Example: decrease in thickness of Y2O3-based intergranular film in AlN is correlated with an increase in bulk thermal conductivity of 24%
More tangible example: lithium phosphate based surficial films on cathode particles can enhance discharge rate

## Slide 34: (My) Final thoughts
Metallurgic thrust during the 1900s: need for better understanding of GB
Several studies on GB for pure metallic systems, binary systems; few on other simpler systems; myriad of important strides were made. However:
  Difficulties in experimentally observing complexion transitions; most measurements are done “indirectly”; many complexions only stable at high temperatures but quenching freezes them at low temperature
  Hard to validate theoretical models, which are already relatively simplistic (they are still difficult to understand, but they don’t account for a lot of stuff) case-by-case basis without a general unifying theory
  Mechanism and kinetics of complexion transitions relatively unknow
More complicated materials (such as solid electrolytes) may have an even larger plethora of complexions and transitions!

## Slide 35: 0-lattice behavior upon translation of lattice 2
Translate crystal 2 by :
Decompose displaced 0-lattice:

## Slide 36: Equivalence between surface energy and tension
Apply a stress to edge of a surface to extend the other edge by
  This stress is equal in magnitude to the surface tension
  Increase in area
  Increase in total energy of surface
  Work done by force
  Surface energy and surface tension are “equivalent”

## Slide 37: Premelting curves
Tang, M., et al. “Diffuse interface model for structural transitions of grain boundaries" Physical Review B 73 024102 (2006).